# BURGERS

(C) 2001 Lauge Fuglsang Nielsen

Content of software:

The software predicts the rheological behaviour of a Burgers body. Any sub-characteristics of the body can be controlled by the user (such as stiffness- and relaxation properties). The software is presented in two versions:

BURG-SCI predicts Complex stiffness (Real and Imaginary), absolute stiffness and loss tangent, creep function and relaxation function. All these properties are of great significance in materials physical science. BURG-SCI operates with time in seconds.

BURG-ENG predicts creep function and relaxation function. Also predicted are these functions in normalized forms – considering un-loading at arbitrary times. BURG- ENG operates with time in days, which is convenient in most structural engineering work.

Note: The Burgers body is the most general model of so-called simple viscoelastic materials. Others (described in the Burgers software) are the Maxwell body, the Kelvin body, the Thomson body, and the Lethersich body. All these bodies can be considered as special cases of the Burgers body. The BURGER software can therefore consider their rheological behaviour. Modifications to introduce for this purpose can be determined from a scheme presented in the software.

References:

The Burgers software is based primarily on results obtained in:

Nielsen, Lauge Fuglsang: "Rheologische Eigenschaften für isotrope linear-viscoelastische Kompositmaterialien", Cement and Concrete Research, 3(1973), 751-766.

Idem: 'Materialemekanik' (Material Mechanics), Text note in Course 59409: Material mechanics and porous materials, Dept. Structural Mechanics and Materials, Technical University of Denmark, 2000.

Idem: 'Materialemekanik II' (Materials Mechanics II), Text note in Course 6110: Rheology, Fracture, Composite materials, and materials lifetime, Report 189, Building Materials Lab., Technical University of Denmark, 1988.

Idem: 'An improved method for estimating the dynamic properties of materials', Sound and Vibration, Instrumentation reference issue, February 2000, 20-24, (co-authors, N.J. Wismer and S. Gade).