Materialenyt 1:2001, DSM (Danish Society for Materials Testing and Research)

Numerical analysis of composite materials

Lauge Fuglsang Nielsen

Abstract: A method is presented in this paper by which mechanical properties such as stiffness, eigenstrain/stress (e.g. shrinkage and thermal expansion), and physical properties (such as various conductivities with respect to heat, electricity, and chlorides) can be predicted for composite materials with variable geometries. A separate analysis of porous materials is made in a special section of the paper with strength estimates added to the list of composite properties considered above. The property of percolation (phase continuity) is also considered.

The paper is not a 'textbook' in composite materials. It is a 'users manual' with operational introductions to the basics and running of the program COMP developed for computer analysis of composite materials. The program, which can be downloaded from the following address, is based on work previously made by the author in the area of composite materials.

http://www.byg.dtu.dk/publicering/software_d.htm.

Introduction

The composites considered in this paper are isotropic mixtures of two components: phase P and phase S. The amount of phase P in phase S is quantified by the so-called volume concentration defined by c = VP/(VP+VS) where volume is denoted by V. It is assumed that both phases exhibit linearity between response and gradient of potentials, which they are subjected to. For example: Mechanical stress versus deformation (Hooke's law), heat flow versus temperature, flow of electricity versus electric potential, and diffusion of a substance versus concentration of substance.

For simplicity – but also to reflect most composite problems encountered in practice – stiffness and stress results presented assume an elastic phase behaviour with Poisson’s ratios (P = (S = 0.2 (in practice (P ( (S ( 0.2). This means that, whenever stiffness and stress expressions are presented, they can be considered as generalized quantities, applying for any loading mode: shear, volumetric, as well as un-axial. This feature is explained in more details in a subsequent section (Composite analysis).

The composite properties specifically considered in this paper are stiffness, eigenstrain (such as shrinkage and thermal expansion), and various conductivities (with respect to chloride or heat flow e.g.) as related to volume concentration, composite geometry, and phase properties: Young's moduli EP and ES with stiffness ratio n = EP/ES, eigenstrains λP and λS, and conductivities QP and QS with conductivity ratio nQ = QP/QS. Normalized strength, S/So, of porous materials is also considered where S and So denote porosity dependent strength and real strength of phase S respectively. Further notations used in the text are explained in the list of notations at the end of the paper.

The composite properties presented in this paper are determined by a general method developed by the author in (,,). The strength of this method, including the present method, relative to other prediction methods with fixed, not variable types of composite geometries (such as plates or fibres in a matrix), is that global (standard) solutions are presented which apply for any isotropic composite geometry. Specific composites are considered in these global solutions by so-called 'geo-functions' (θ) where specific geometries are quantified by so-called 'shape functions' (μP,μS). Thus, properties can be predicted where geometry can be respected as it really develops in natural or man-made composite materials.

Not to exaggerate our present knowledge of composite geometries it has, deliberately, been chosen to keep the shape functions (μ) described by simple mathematical expressions defined by only three geometrical parameters (two shape factors and one critical concentration, see Equation 2). It is emphasized, however, that the complexity of shape functions does not influence the global property predictions previously referred to. As more knowledge on the description of composite geometry turns up as the result of new research we just introduce the more 'accurate' shape functions.

It is emphasized that the paper is not a "textbook" in composite materials. The text is rather brief, and no attempts have been made to explain expressions theoretically. The paper should rather be considered as a 'users manual': An operational introduction to the basics and application of the computer program COMP, which can be downloaded from http://www.byg. dtu.dk/publicering/software_d.htm.

Geometry

As demonstrated in Figure 1 composite geometry can be described by so-called shape functions which are determined by so-called shape factors (μPo,μSo) and critical concentrations, cP and cS ( cP: Shape factors tell about the shapes of phase components at dilute concentrations. Critical concentrations are concentrations where the composite geometry changes from one type to another type.

1

Figure 1. Geometrical significance of shape functions. (μP,μS) = (+,-) means discrete P in continuous S. (μP,μS) = (+,+) means mixed P in mixed S. (μP,μS) = (-,+) means continuous P with discrete S. Black and white signatures denote phase P and phase S respectively.

At fixed concentrations we operate with the following types of composite geometries: DC means a discrete phase P*) in a continuous phase S. MM means a mixed phase P geometry in a mixed phase S geometry, while CD means a continuous phase P mixed with a discrete phase S. We notice that MM-geometries (if porous) are partly impregnable. In modern terminology this means that phase P percolation exists in composites with c > cS. Percolation is complete for c ( cP. Porous materials have lost any coherence in this concentration area with no stiffness and strength left.

Composite geometries may change as the result of volume transformations associated with increasing phase P concentration. We will think of changes as they are stylised in Figure 1: At increasing concentration, from c = 0, discrete P elements agglomerate and change their shapes approaching a state at c = cS where they start forming continuous geometries. Phase P grows fully continuous between c = cS and c = cP such that the composite geometry from the latter concentration has become a mixture of discrete, de-agglomerating, phase S particles in a continuous phase P.

Figure 3. Composite Spheres Assemblage with phase S particles, CSAS.

Figure 2. Composite spherical assemblage with phase P particles, CSAP.

In a complementary way the geometry history of phase S follows the history of phase P and vice versa. The geometries just explained can be shifted along the concentration axis. A composite may develop from having a DC geometry at c = 0 to having a MM geometry at c = 1. Such composite geometries, with cP > 1 and 0 < cS < 1, are named DC-MM geometries. Other composites may keep their DC type of geometry all the way up to c = 1 in which case the composite geometry is denoted as a DC-DC geometry, with both critical concentrations > 1. The geometry outlined in Figure 1 changes from DC to CD geometry which makes it a DC-CD geometry with both critical concentrations in c = 0-1.

Ideal geometries at c = 0 and at c = 1 of a DC-CD composite are illustrated in Figures 2 and 3 respectively. We notice in this context that the composite theory developed in (1,2,3) is based on the concept that any isotropic composite geometry is a station on a geo-path moving from the CSAP geometry shown in Figure 2 to the CSAS geometry shown in Figure 3. CSA is an abbreviation for the composite model Composite Spheres Assemblage introduced by Hashin in (). It is noticed that the four letter symbols for composite geometries are subsequently also used in the meaning, a 'DC-CD type of composite' or just a 'DC-CD composite'.

Quantification of composite geometry

The various types of geometries considered are listed in Figure 4 which defines the following two composite classes considered in this paper: Particulate composites are defined by the former row. They have particles in a matrix geometry (DC) at small concentrations. Lamella composites are defined by the latter row. They have a mixed phase P geometry in a mixed phase S geometry (MM) at low concentrations. Obviously, the phenomenon of percolation previously considered develops between the two critical concentrations. In Figure 4 the phase P percolation is indicated by grey shadings. We assume that percolation varies linearly from being 0 at c < cS to being 100% at c > cP.

Figure 4. Composite types versus critical concentrations. Former and latter two letters denote composite geometry at c = 0 and at c = 1 respectively.

Shape factors and geo-paths

Shape factors for composites in general can be estimated from the geo-path graph presented in Figure 5 reproduced from (,3). The geometries passed when the phase P concentration increases from c = 0 to c = 1 are shown in this figure. Plain fibre/disc shape factors indicated by numbers in Figure 5 are accurately determined by Equation 1, reproduced from (3)**), where particle shapes are quantified by the aspect ratio, A = length/diameter of particle. Spherical particles have A = 1. Long particles have A > 1. Flat particles have A < 1.

(1)

2

Figure 5. Geo-path and tentative description of shapes: Numbers indicate fibre aspect ratio A of particles (Equation 1). Frame- and fibre works are agglomerating MM-structures of long crumbled fibres and shorter crumbled fibres respectively. Disc works are agglomerating MM-structures of crumbled discs (sheets). Plate works are crumbled sheets (foils).

Remark: For particulate composites with phase P being a mixture of particles with various aspect ratio distributions the shape factors can be accurately calculated by a method developed in (3). For the case of mixtures with only two aspect ratios this method is simplified to be part of the program COMP previously referred to. An example: A mixture made with 20% A = 0.3 and 80% A = 2 is characterized by the shape factors (μPo,μSo) = (0.83,-0.68).

Critical concentrations

It is emphasized that the critical concentrations depend very much on the processing technique used to produce composites. We notice that particle size distribution is part of processing. For particulate composites, for example, the critical concentration cS can be thought of as the concentration at first severe interference of phase P (starting the creation of a contInuous skeleton). Improved quality of size distribution (smoothness and density) is considered by increasing cS. At this concentration porous materials become very stiff when impregnated with a very stiff material. At the other critical concentration, c = cP, the composite becomes a mixture of phase S elements completely wrapped in a matrix of phase P. As previously mentioned porous materials loose their stiffness and strength at cP because phase P has become a continuous, enveloping, void system.

| TYPE | Crit-con cS | EXAMPLES |
| --- | --- | --- |
|  | DC | cS > 1 | Particulate composite (concrete, mortar). Extremely high quality of grading (approaching CSAP composites). Pore system: Not impregnable. Finite stiffness at any porosity |
| DC | MM | 1 > cS > -μSo/μPo | Particulate composite (concrete, mortar) with particle interference at c = cS. Increasing quality of grading is quantified by larger concentration cS at first severe interference. Pore system: Only impregnable for porosities c > cS. Finite stiffness at any porosity. |
|  | CD | -μSo/μPo > cS > 0 | Mixed powders (ceramics). Pore system: Only impregnable for porosities c > cS. No stiffness for porosities c > cP. |
|  | MM | -μSo/μPo > cS | Mixed lamella/foils ("3D-plywood"). Pore system: Fully open at any porosity. Finite stiffness at any porosity. |
| MM | CD | 0 > cS > -μSo/μPo | Mixed lamella/foils ("3D-plywood"). Pore system: Fully open at any porosity. No stiffness for porosities c > cP. |

Table 1. Range of critical concentrations applying for various composites.

Remark: The definition of interference ('severe') introduced above is kept throughout the paper. It is implicitly assumed that particles at c > cS are kept together by a very thin, sufficiently strong matrix "glue".

As previously indicated, critical concentrations can be fictitious (outside c = 0 - 1). In such cases they do not, of course, have the immediate physical meanings just explained. Theoretically, however, if we think of the c-axis as a plain geometry axis we may keep the explanation given in order to describe in an easy way how the rate of changing the composite geometry is influenced by the processing technique used. In such fictitious cases critical concentrations will have to be estimated from experience, or detected from calibration experiments.

Preparation of composite analysis

The preparation of a composite analysis by COMP is as follows:

-	Estimate shape factors (μPo,μSo) from Figure 5 - or calculate by Equation 1 if phase P are plain discs/fibres. (We re-call that shape factors for two-shape mixtures can be determined by a special subroutine included in COMP).

-	Then decide the critical concentration cS (or cP) from knowing about mixing technology and observations made on geometrical formation.

-	This information quantifies the composite geometry by the so-called shape functions expressed by Equation 2.

Remark: We recall from the introductory section of this paper: Shape functions are deliberately expressed by simple mathematical expressions in order not to predict properties with an 'accuracy' out of proportions to what is actually know about composite geometry. A consequence of such simplification is that the quantities of (μPo,μSo) and (cS or cP) chosen above must be adapted to each other such that the critical concentration not chosen is predicted realistically by Equation 2. Figure 4 and Table 1 are useful when deciding on realistic shape functions for practical composite analysis.

(2)

-	The last step of preparing a composite analysis by the global solutions (valid for any geometry) presented in Equations 4 to 8 is to calculate the so-called geo-functions expressed by Equation 3 for stiffness analysis and conductivity analysis respectively.

(3)

Composite analysis

With composite geometry described by the geo-functions presented in Equation 3 a property analysis can now be made using the following glob-al solutions 4 – 8 with symbols explained in the list of notations presented at the end of the paper.

In general phase P and phase S stresses presented are volume averages. Accurate local stresses can only be determined for very special composites. One such case is of special interest for practice, namely the maximum tensile phase S stress in a CSAP composite subjected to eigenstrain (think of shrinkage cracking in concrete). The software COMP previously referred to includes this accurate prediction.

Remark: We re-call from the introduction that the stiffness- and stress expressions presented have a generalized meaning. They can be used for any loading mode, shear, volumetric, as well as uni-axial. For example, E/ES can also be used to predict the composite shear modulus, G/GS, and the composite bulk modulus, K/KS, normalized with respect to the phase S properties. In a similar way the phase stresses, (P/( and (S/(, also apply independently of loading mode as long as both phase stress modes ((P,(S) and composite (external) stress modes (() are the same.

Six examples of composite analysis (by COMP) are demonstrated in a following section.

Stiffness and eigenstrain/stress

Stiffness

(4)

Stress due to external mechanical load

(5)

Eigenstrain - linear

(6)

Eigenstress – hydrostatic

(7)

Conductivity

(8)

Bounds on stiffness and conductivity

It comes from (1,2,3) that the above predictions are bounded as follows between the exact solutions for the CSA composite illustrated in Figures 2 and 3.

(9)

The stiffness bounds are obtained introducing θ ( 1 and θ ( n respectively into Equation 4. The conductivity bounds are obtained introducing θQ ( 2 and θQ ( 2nQ respectively into Equation 8. The bounds such determined are the same as can be obtained from the studies made by Hashin and Shtrikman in () on composite stiffness and in () on composite conductivity. The bounds just considered are subsequently referred to by H/S.

(10)

Porous materials

Porous materials can be analysed elastically by the expressions already presented, just by introducing a stiffness ratio of n = 0. In a similar way conductivity can be determined introducing a conductivity ratio of nQ = 0 (assuming a void conductivity of QP = 0). The results are the following very simple expressions which are the basics of the computer program POROUS (in the COMP package). It is noticed that e and q become 0 for c > cP.

(11)

Strength estimate

An algorithm is included in POROUS by which a first estimate of strength of porous materials can be made by the semi-empirical expression presented in Equation 12 (with S/So ( 0 for c > cP).

(12)

Porosity dependent strength and strength at very low porosity are denoted by S and So respectively. It is emphasized that So is the real strength, not the theoretical strength, of phase S.

The strength expression is based on the following arguments: Strength at low porosities is as predicted by the so-called MOE-MOR relation (Modulus Of Elasticity - Modulus Of Rupture) presented in Equation 13 and illustrated in Figure 6. This relation was developed in (,) for materials with cracked uni-sized spherical pores.

At increasing porosities most real pore systems will become more flexible with respect to geometry then described by the spherical pore model just mentioned. Increased flexibility will reduce interaction such that strength reduction will become less serious than described by Equation 13. Keeping the low porosity quality of Equation 13, this feature is considered by Equation 12 letting it describe strength in a similar way as has previously been proposed from experimental observations made by, for example, Ryshkewitch (,), Balshin (), and Hasselman (), who suggested strength to decrease exponentially, parabolically, and linearly respectively with respect to porosity

(13)

Figure 6. MOE-MOR relation for a material with uni-sized spherical pores with co-centric cracks.

Parameter deduction from experiments

Data from stiffness tests on porous materials can be used to determine ES, μPo, and cP: We linearize the former expression of Equation 11 as shown in Equation 14. Then μPo, cP, and ES are easily deduced by linear regression of the manipulated experimental data (X,Y), optimising the fit quality with respect to cP.

(14)

Now other material quantities like QS and So (and the factor 3/4 in Equation 13 eventually) can be deduced in similar ways by linear regressions of manipulated experimental data.

Examples

Some examples (exercises) are presented in this section where composites are subjected to a property analysis as it has been presented in this paper. The text of the examples is very short. Only information absolutely necessary for solving the problems is presented. Discussion of the solutions is left to the reader herself. Among the composites considered are the DC-MM and DC-CD composites represented by their shape functions shown in Figures 7 and 8 respectively, compare with Figures 1 and 4.

Figure 7. Geometry of 'soft concrete' considered in Example 1.

Figure 8. Geometry of cement paste considered in Example 2.

The examples are treated numerically by the computer program package, COMP. The (main) program, NORMAL, is meant for composites with components the geometries of which are flexible (phase geometries adjust to each other, naturally, by compaction, or otherwise). The algorithm of this program follows exactly the text previously presented in this paper.

Some composites, such as concrete, however, form a stable phase P skeleton at the critical concentration cS such that voids will inevitably show up at higher concentrations. The program, NO-FLEX is a modification of NORMAL developed in (3) which considers the reducing effect of self-inflicted voids on properties by a simple 'freezing' of shape functions such that these become constants for c > cS for which concentrations phase S is porous. It is implicitly assumed in such modification that particles at c > cS are kept together by a thin, sufficiently strong matrix "glue".

Except for a few composites the above discussion on NO-FLEX is of minor interest for practice. Most often we do not need other programs than NORMAL because we have no interest in producing composites with self-inflicted voids. The exceptions are composites, such as light clinker concrete, where voids are wanted to satisfy an overriding demand for heat insulating property, irrespective of stiffness lost.

In summary: The program NORMAL can be used for the analysis of most composites considered in practice. Only very special composites (with self created voids) need analysis by the alternative programs presented. Finally, a special program (POROUS) considers the mechanical/physical behaviour of porous materials, including strength estimates.

Example 1: 'Soft concrete’:

Stiffness, internal stress, and eigenstrain/stress

Components: Phases (P,S) = (aggregates, cement paste). Young's moduli: (EP,ES) = (1000,30000) MPa. Linear eigenstrain (negative shrinkage): (λP,λS) = (0,-0.001).

Figure 9. Example 1: Composite stiffness.

Figure 10. Example 1: Internal stress caused by external mechanical load.

Figure 11. Example 1: Linear composite eigenstrain (negative shrinkage).

Figure 12. Example 1: Hydrostatic stress caused by shrinkage of matrix (S).

Geometry, see Figure 7: Phase P is a mixture of fibres and discs such that (μPo,μSo) = (0.6,-0.3), (corresponding, approximately, to equal amounts of aggregates with aspect ratio A = 5 and aggregates with A = 0.2). The mixture has a critical concentration of  cS = 0.75.

Analysis: Software NORMAL. A production technique is assumed by which phase P can be considered flexible. Otherwise predictions should be made using NO-FLEX.

Example 2: Cement paste system:

Stiffness and Chloride diffusion

Components: Phases (P,S) = (saturated capillary pores, cement gel). Young's moduli: (EP, ES) = (0,32000) MPa. Chloride diffusion coefficients: (QP,QS)/QP = (1, 0.00008) with QP = 2*10-9 m2/sec.

Geometry, see Figure 8: Aggregates (pores) aspect ratio at low c: Estimate A = 4 ( (μPo,μSo) = (0.81,-0.25). Critical concentration: cP = 0.78 corresponding to cS = 0.24, see Equation 2, (it has been shown in () that cement paste exhibits no stiffness (and strength) at porosities greater than c ( 0.78 which means that the solid phase (S) becomes surrounded by voids at that concentration, defining cP).

Figure 14. Example 2: Chloride diffusivity of cement paste as related to capillary porosity.

Figure 13. Example 2: Stiffness of cement paste as related to capillary porosity.

Analysis: Software NORMAL.

Experimental data: Stiffness: (,). Conductivity: (,).

Example 3: Light clinker concrete:

Stiffness and heat conductivity

Components: Phases (P,S) = (clinker, cement paste). Young's moduli: (EP,ES) = (8,25) GPa. Heat conductivities: (QP,QS) = (0.2,1.2) J/(s*(K* m). Densities: (dP, dS) = (900,2000) kg/m3.

Figure 15. Example 3: Stiffness of light clinker concrete. Non-flexible phase P.

Figure 16. Example 3: Stiffness of light clinker concrete. Non-flexible phase P.

Figure 17. Example 3: Heat conductivity of light clinker concrete. Non-flexible phase P.

Figure 18. Example 3: Heat conductivity of light clinker concrete. Non-flexible phase P.

Geometry: Clinker aggregates with A ( 1. Critical concentration cS ( 0.6.

Analysis: Software NO-FLEX.

Experimental data: Stiffness versus density: ()

Example 4: Cement mortar: Stiffness

Components: Phases (P,S) = (quartz sand, cement paste). Young's moduli: (EP, ES) = (75,25) GPa.

Geometry: Phase P consists of compact, nearly uni-sized particles which interfere at cS = 0.55. It can be assumed that A = 1.

Analysis: Software NO-FLEX.

Experimental data: Stiffness ()

Figure 19. Example 4: Stiffness of cement mortar with quartz sand.

Example 5: Hardened cement paste:

Stiffness and first estimate of strength

Components: A HCP is looked at with phase P considered to be the total pore system (gel + capillary pores) in a phase S of gel solid. The stiffness data shown in Figure 20, reproduced from (), represent stiffness for such a system. The experimental data are from (). The theoretical data are as predicted in (21) by a method similar to the one presented in this paper. A solid gel stiffness of ES = 80000 MPa was deduced from the experimental stiffness data, see Equation 14, together with the geometrical parameters μPo = 0.33 and cP ( 1.

Figure 20. Example 5: Young's modulus of hydrated Portland cement paste (HCP).

Figure 21. Example 5: Compressive strength estimate of HCP. Experimental data, with So ( 450 MPa, are introduced as explained in the main text.

The experimental strength data for HCP shown in Figure 21 are from ( as evaluated in 14). No geometrical data could be deduced from the data reported in (23) except that cP ( 0.78. The theoretical strength data shown in Figure 21 are predicted by Equation 12 with shape factors estimated to be of the same orders of magnitude as for the HCP in Figure 20.

Analysis: Software POROUS.

Example 6: Hashin and Budiansky: Stiffness

It is up to the reader herself to show that the method presented in this paper correctly predicts the Hashin's (4) stiffness expression (left side in Equation 9) with (μPo,μSo,cS) = (1,-1,() corresponding to (A,cS) = (1,(). The reader may also show that the Budiansky's () stiffness expression reproduced in Equation 15 is correctly predicted with (μPo,μSo,cS) = (1,-1,0.5) corresponding to (A,cS) = (1,0.5).

(15)

Final remarks

Isotropic composites of various geometries are considered in this paper. A computer analysis of the mechanical/physical properties of such materials is prepared and developed on the basis of the authors theoretical work (1,2,3) in the field of composite materials. Examples of using the program developed (COMP) confirm the general observation made in (1,2,3) that a very satisfying agreement exist between theoretically predicted data and experimentally obtained data reported in the composite literature.

Special sub-programs are prepared to consider particulate composites with non-flexible particles - and strength of porous materials.

It is emphasized that the basic prediction expressions presented are global, meaning that they apply for any isotropic composite geometry. Thus, other composites than those explicitly considered in this paper can be analysed using the same expressions. This feature can be further studied in (3,) where it is also demonstrated how the prediction method can be generalized to include viscoelastic composite properties. A simple version of such generalization has recently been applied by the author (,,,) to study the rheology of extreme composites such as Self Compacting Concretes.

Notations

Abbreviations and subscripts

V	Volume

P	Phase P

S	Phase S

no subscript		Composite material

H/S	Hashin/Shtrikman's property bounds

Geo-parameters

c = VP/(VP+VS)	Volume concentration of phase P

μo	Shape factor

μ	Shape function

cP,cS	Critical concentrations

θ	Geo-function for stiffness

θQ	Geo-function for conductivity

Density

d	Phase density

d = c*dP+(1-c)*dS	Composite density

Stiffness and other properties

E	Stiffness (Young's modulus)

e = E/ES	Relative stiffness of composite

n = EP/ES	Stiffness ratio

Q	Conductivity (eg. thermal, electrical, chloride)

q = Q/QS	Relative conductivity of composite

nQ = QP/QS	Conductivity ratio

λ	Linear eigenstrain (eg. shrinkage, thermal expansion)

Δλ = λP-λS	Linear differential eigenstrain

Stress

σ	External mechanical stress

σP	Phase P stress caused by external mechanical stress

σS	Phase S stress caused by external mechanical stress

ρ	Hydrostatic stress caused by eigenstrain

Strength of porous material

S	Porosity dependent strength

So	Real strength (0-porosity) of phase S in porous material

Non-flexible phase P especially

ca = (c-cS)/c/(1-cS)	Phase S porosity (for c > cS)

cPOR = (c-cS)/c		Porosity (of composite) for c > cS

Literature

# Footnotes

*)	A phase with continuous geometry (C) is a phase in which the total composite can be traversed without crossing the other phase. This is not possible in a phase with discrete geometry (D). A mixed geometry (M) is a continuous geometry with some discrete elements.

**)	Modified version of a similar expression presented in (2).

# Endnotes

.	Nielsen, L. Fuglsang: "Elastic Properties of Two-Phase Materials", Materials Science and Engineering, 52(1982), 39-62.

.	Idem: "Stiffness and other physical properties of composites as related to phase geometry and connectivity - Part I: Methods of analysis" and "- Part II: Quantification of Geometry”, 3rd Symposium on Building physics in the Nordic countries, Copenhagen, sept. 13-15, 1993, pages 725-734 and 735-743 in Proceedings Vol 2 (Ed. B. Saxhof), 1993,

.	Idem: "Composite Materials - Mechanical and physical behaviour as influenced by phase geometry", Monograph, Department of Civil Engineering, Tech. Univ. Denmark, in press 2002.

.	Hashin, Z.: "Elastic moduli of heterogeneous materials". J. Appl. Mech., 29  (1962), 143 - 150.

.	Nielsen, L. Fuglsang: "Composite materials with arbitrary geometry", Text note for Summer school on 'Hydration and Microstructure of High Performance Concrete' at the Dept. Struct. Eng. and Materials, Techn. Univ. Denmark, Lyngby, August 16-25, 1999.

.	Hashin, Z. and Shtrikman, S.: "Variational approach to the theory of elastic behaviour of multi-phase materials". J. Mech. Solids, 11(1963), 127 - 140.

.	Idem: "A variational approach to the theory of the effective magnetic permeability of multiphase materials", J. Appl. Phys. 33(1962), 3125.

.	 Nielsen, L. Fuglsang: "Strength and stiffness of porous materials". Journ. Am. Ceramic Soc. 73(1990), 2684-2689.

.	Idem: "Strength of porous material - simple systems and densified systems", Materials and Structures, 31(1998), 651-661.

.	Ryshkewitch, E.: "Compression Strength of Porous Sintered Alumina and Zirconia". Journ. Am. Ceram. Soc., 36(1953), 65 - 68.

.	Duckworth, W.: "Discussion of Ryshkewitch Paper". J. Am. Ceram. Soc. 36(1953), 68. (Ryshkewitch, E.: "Compression Strength of Porous Sintered Alumina and Zirconia". J. Am. Ceram. Soc. 36(1953), 65 - 68).

.	Balshin, M.Y.: "Relation of mechanical properties of powder metals and their porosity and the ultimate properties of porous metal-ceramic materials". Dokl Akad Nauk SSSR 67/5/(1949).

.	Hasselman, D.P.H.: "Relation between effects of porosity on strength and on Young's modulus of elasticity of polycrystalline materials", J. Am. Ceram. Soc., 46(1963), 564 - 565.

.	Nielsen, L. Fuglsang: "Strength developments in hardened cement paste – Examination of some empirical equations", Materials and Structures, 26(1993), 255-260.

.	Beaudoin, J.J. and R.F. Feldman: "A study of mechanical properties of autoclaved Calcium silicate systems", Cem. Concr. Res., 5(1975), 103-118.

.	Feldman, R.F. and J.J. Beaudoin: Studies of composites made by impregnation of porous bodies. I. Sulphur impregnant in Portland cement systems", Cem. Concr. Res., 7(1977), 19-30.

.	Bentz, D.P., Jensen, O.M., Coats, A.M., and Glasser, F.P.: "Influence of Silica Fume on diffusivity in cement-based Materials. Part I: Experimental and computer modelling studies on cement pastes", Submitted to Cement and Concrete Research 1999.

.	Mejlhede Jensen, O.: Chloride ingress in cement paste and mortar measured by Electron Probe Micro Analysis", Report R51(1999), Dept. Struct. Eng. and Materials, Tech. Univ. Denmark.

.	Palmus, L.: "Letklinkerbetons mekaniske egenskaber" (in danish, Mechanical properties of light clinker concrete), M.Sc. thesis, Spring 1996, Dept. Struct. Engineering and Materials, Tech. Univ. Denmark.

. 	Ishai, O.: ”Influence of sand concentration on deformations of mortar beams under low stresses”, ACI Journ., Proceedings 58(1961), 611-622.

.	Nielsen, L. Fuglsang: "Elasticity and Damping of Porous Materials and Impregnated Materials", Journ. Am. Ceramic Soc., 67(1984), 93 - 98.

.	Helmuth, R.A. and D.H. Turk: "Elastic moduli of hardened Portland cement and Tricalcium silicate pastes: Effects of porosity", pp. 135-144 in Symposium on structure of Portland cement and concrete. Highw. Res. Bd., Spec. Rept., No. 90, 1966.

.	Bergström, S.: “Lagringstemperatur, Lagringstid och Betonghålfasthet” (‘Curing temperature, curing time, and strength of concrete’), Medd. No. 27, Cement och Betong Institutet, Stockholm 1953.

.	Budiansky, B.: On the elastic moduli of some heterogeneous materials". J. Mech. Phys. Solids, 13(1965), 223 - 227.

.	Nielsen, L. Fuglsang: "Materialemekanik" (in danish, Material mechanics), Text note for Course 59409: Material mechanics and porous materials, Dept. Struct. Eng. and Materials, Tech. Univ. Denmark, 2000.

.	Idem: "Rheology of extreme composites", In "Papers in Structural Engineering and Materials - A Centenary Celebration", 179-187, Dept. of Struct. and Materials, Tech. Univ. Denmark, 2000.

.	Geiker, M.R., Brandl, M., Trane, L. Nyholm, and Nielsen, L. Fuglsang: "Effect of coarse aggregate fraction and shape on the rheological properties of self-compacting concrete". Cement, Concrete, and Aggregates, Vol. 24(2002), No. 1.

.	Nielsen, L. Fuglsang: "Generalized Bingham description of fresh concrete", XVIII Symposium on Nordic Concrete Research in Helsingør, Denmark, 12-14 June 2002. Proceedings, Danish Concrete Society 2002, 120-122.

.	Nielsen, L. Fuglsang: "Rheology of some fluid extreme composites - such as self-compacting concrete", Nordic Concrete Research, 2(2001), 83-93.