CRACK

( 2000 Lauge Fuglsang Nielsen

The software CRACK is developed during the preparation of the following two publications.

Nielsen, L. Fuglsang: 'Modified Dugdale cracks – some easy crack relations', Report R-38 (1997), Dept. Struct. Eng. and Materials, Technical University of Denmark, 1997

Abstract: The Dugdale crack model is widely used in materials science to predict strength of defective (cracked) materials. A stable Dugdale crack in an elasto-plastic material is prevented from spreading by uniformly distributed cohesive stresses acting in narrow areas at the crack tips. These stresses are assumed to be self created by local materials flow. The strength σCR predicted by the Dugdale model is σCR = (EΓCR/πl)1/2 where E and l are Young's modulus and crack half-length respectively of the material considered. The so-called critical strain energy rate is ΓCR = σLδCR where σL is strength, and at the same time constant flow stress, of the un-cracked material while δCR is flow limit (displacement).

Obviously predictions by the Dugdale model are most reliable for materials with stress-strain relations where flow can actually be described (or well approximated) by a constant flow stress (σL). A number of materials, however, do not at all exhibit this kind of flow. Such materials are considered in this paper by Modified Dugdale crack models which apply for any cohesive stress distribution in crack front areas. Formally modified Dugdale crack models exhibit the same strength as a plain Dugdale model. The critical energy release rates ΓCR, however, become different. Expressions (with easy computer algorithms) are presented in the paper, which relate critical energy release rates and crack geometry to arbitrary cohesive stress distributions.

For future lifetime analysis of viscoelastic materials strain energy release rates, crack geometries, and cohesive stress distributions are considered as related to sub-critical loads σ < σCR. Such information needed in viscoelastic analysis is not obtained from traditional stress-deformation tests on materials.

Limitations of the expressions presented are discussed. They are the same as for the well-known Griffith load capacity, namely: predicted σCR must be lower than σL/3. The reason is that ΓCR looses its meaning of an independent material property at higher strengths. A more general strength expression applying at any strength predicted is suggested introducing a so-called characteristic micro structural dimension, which captures the materials failure properties in a more efficient way than ΓCR, does.

Identification of a characteristic micro structural dimension will cause that the rationale behind traditional ΓCR-determination by stress-deformation tests has to be modified. It is therefore suggested that future research on strength should include characteristic micro structural dimensions as a separate topic.

Keywords: Modified Dugdale crack model, cohesive stress, strain energy release rate, stress intensity factor, crack opening, characteristic micro structural dimension, strength, critical load, subcritical load

Nielsen, L. Fuglsang: 'Modified Dugdale cracks and fictitious cracks - subjected to sub-critical loading', Bygningsstatiske Meddelelser, 70(1999), 85-106.

Abstract: The so-called Dugdale/Barenblatt theory to strength determination of cracked materials is adapted such that it can be used in a complete and consistent analysis of the behaviour of cracks when the material is subjected to subcritical loads (less than the materials immediate, un-cracked, strength). 'Consistent' means that the respective cohesive stress histories are parts of a global, experimentally determined cohesive stress-displacement graph.

To the best knowledge of the author such analysis has not yet been made although this step of analysis is probably the most important one with respect to design of real structural members. These carry loads, which are, of course, considerably smaller than the failure load.

Cracked viscoelastic materials (such as cementitious materials) will fail when subjected to any load, including subcritical loads. Due to creep, failure becomes a time dependent phenomenon. Upper and lower bounds for the time to failure initiation are determined in this paper. It is hereby made probable that the true time to failure initiation comes closest to the upper bound solution. Estimates made by traditional means (strain energy release rate considerations) are absolute lower bound solutions.

The assumption made in most theoretical analysis that material properties are genuine (inherent, time-independent properties) is somewhat hard to maintain in practice. The paper demonstrates that measured strength of cracked materials is creep dependent such that a significant gain in measured strength can easily be obtained decreasing the testing time from a couple of minutes to less than a second.

Basically the paper is written with no special material in mind. Examples, however, are based on material properties deduced from the literature on hardened cement paste (HCP). Some new aspects are revealed on the strength of cracked materials, which are not yet considered by experiments. Hopefully the paper may inspire to further experimental work on the influence of creep on the strength of subcritically loaded HCP and other cementitious materials.

Finally, a method is outlined in the paper by which bounds for the total lifetime (time to failure initiation + time for propagating cracks to reach their critical lengths) can be determined for subcritically loaded cracked materials.

Sammenfatning: Revnede materialers adfærd under sub-kritisk belastning (< materialestyrken) undersøges i denne artikel. Den praktiske relevans af en sådan undersøgelse er oplagt. Enhver konstruktion vil i brugstilstand naturligvis stå med spændinger, der ligger under de, der fremkalder brud. Det teoretiske grundlag i artiklen er en tillempet Dugdale/Barenblatt teori med arbitrær sammenhængsspænding i revnefronter.

Det specielle problem, der løses i artiklen kan formuleres: Hvordan opfører et materiale sig, når der med fuld ret kan forlanges konsistens mellem sammenhængsspændingerne ved enhver sub-kritisk belastning. Det vil sige, at sammenhængsspændingen ved enhver sub-kritisk belastning skal kunne beskrives som del af en global sammenhængsspænding, nemlig den eksperimentelt bestemte, der under navnet 'stress-displacement graph, anvendes til bestemmelse af den så-kaldte kritiske tøjnings-energi-hastighed.

Revnede viskoelastiske materialer (som f.eks. cementbaserede) vil bryde sammen under enhver belastning, inklusive sub-kritiske laster. Grundet krybning er styrken blevet et tidsafhængigt fænomen. Grænser opstilles i artiklen for tiden til begyndende krybningsbrud, det vil sige tiden til begyndende revneudbredelse/materialenedbrydning. Det sandsynliggøres, at den sande tid til begyndende krybningsbrud ligger nærmest den øvre grænse. Det vises, at den tid, der normalt bliver skønnet (hvis overhovedet) på grundlag af tøjnings-energi-hastighedens udvikling, er en absolut nedre grænseværdi.

Det vises, at krybningens indflydelse på målt 'styrke' kan være så udpræget, at en betydende styrkegevinst nemt kan opnås ved at reducere prøvetiden fra nogle minutter til under et sekund.

Grundlæggende er artiklen skrevet uden tanke på et bestemt materiale. I eksemplerne er der imidlertid tænkt på hærdnet cementpasta (HCP). Der afsløres her visse forhold, der hidtil ikke har været belyst eksperimentelt. Forhåbentlig vil artiklen i den henseende inspirere til levetidsstudier af sub-kritisk belastet HCP - og krybning i revnefrontsområder.

Afslutningsvis skitseres en metode med hvilken grænser for den totale materiale-levetid (tid til katastrofebrud) kan bestemmes.