POLEDRY

Lauge Fuglsang Nielsen

A software 'POLEDRY" has been developed by the author which predicts the stress states as they develope in a trunk during drying.

The software is based on the following two papers, from which the subsequent quotations are reproduced.

Nielsen, Lauge Fuglsang: "Drying of wood, Part I: Stresses caused by drying", Bygningsstatiske Meddelelser, 57(1986), 73-100.

Idem: "Drying of wood, Part II: Damage free drying", Bygningsstatiske Meddelelser,  57(1986), 101-115.

# ….. Crack growth in wood is promoted by drying. This phenomenon is unfortunate because cracks may reduce strength considerably. It is well known that fast drying is more severe in this respect than slow drying. This observation is the basis of any empirical rule, which has been suggested in drying technology to optimize economy (time) and quality of wood.

….. The scope of this paper is to illustrate theoretically that there is a "safe" rate of drying below which the original structure of wood can be maintained. This means that the inherent defect nuclei in wood will not grow into real cracks. We consider round poles being dried from a moisture content which initially is uniformly distributed at a level lower than or equal to the one defined by the fiber saturation point (25 - 30%). The potential cracks (to avoid) are those having a leading edge parallel to the pole axis and a radial direction of propagation.

……The pole material is modeled in the traditional way, meaning that assumptions are made implying cylindrical homogeneity and orthotropy as related to the pole axis. Accurate elastic stress-strain solutions are first established which are then converted to their viscoelastic counterpart solutions assuming that the mechanical behavior of wood can be described linear-vIscoelastically according to the Power Law description). It is hereby demonstrated how creep considerably reduces the ‘dangerous’ tangential surface stresses, which are the results of a traditional elastic analysis.

….. We recall that we have considered especially the areas at the surface of a pole. This should be kept in mind when evaluating the statements made on drying with damage. For example, the pole considered does not necessarily lose its strength totally when deep cracks appear at the surface. The first cracks developed may very well produce a stress relaxation inside the pole, which reduces the chances that damage will occur in this area. Mathematically the drying problem of wood components with propagating cracks is extremely difficult to solve. This has already been indicated in the preceding section.

It is, however, very satisfactory that the drying process which leaves wood with its best end-quality is accessible for analysis. This paper has given an example of that: Poles drying as shown in Figure xx. Other examples, involving other cross-sections and moisture histories may be analyzed in exactly the same way.

## Remarks

It is noticed that any subject considered in the papers is not handled by the software (POLEDRY) presented. The program, however, can easily be modified to do so.

# Footnotes

) Nielsen, Lauge Fuglsang: "Power Law creep as related to relaxation, elasticity, damping, rheological spectra and creep recovery - with special reference to wood", Conf. of Int. Union of Forestry Research Organizations (IUFRO), Xalapa, Mexico, Dec. 1984, Proc., Build. Mat. Lab., Tech. Univ. Denmark 1985, 181 - 204.

Idem: "Power Law creep of wood - moisture variations aspects", Timber Engineering Conference (International Union of Forest Research Organizations); Bordeaux, France, Aug. 17-21, 1992, Proc., Build. Mat. Lab., Tech. Univ. Denmark 1992, 123 - 134