Generalized Bingham description of fresh concrete

Lauge Fuglsang Nielsen

Associate professor, Ph.D.

Department of Civil Engineering, Building 118

Technical University of Denmark

DK-2800 Lyngby, Denmark

E-mail: lfn@byg.dtu.dk

Abstract

A method is presented by which the well-known Bingham description of flow in homogeneous liquids with yield stress can be generalised to apply also for composite fluids. In the present context such fluids are defined as traditional Bingham fluids mixed with very stiff particles of known shapes and size distributions. In practice the composite aspects of the generalised Bingham description is a major advantage. Only a few geometrical parameters for the particles and two material properties for the fluid matrix are required in order to describe the Bingham behaviour of any composition of the composite fluid considered. The Bingham method normally used needs experimental calibration for any new composition.

Due to the very strict space limits for papers to this conference the generalization method just outlined is presented as an operational summary of a detailed study on the rheology of fluid composites recently reported in [1]. In the present paper composites thought of are self-compacting concretes (SCC) modelled as aggregates in a fluid matrix of cement paste (or mortar)2.

Key words: Composite fluid, Bingham, Composite Bingham, Self-compacting concrete (SCC)

Introduction and theoretical results

(1)

(2)

The prime scope of this paper is to look at possibilities of establishing a composite method of predicting the rheology of SCC, which may serve as an alternative to the semi-empirical method, suggested by deLarrard [2]. The theoretical basis of doing so has recently been developed in [1] from which the following presentation is summarized: The composite fluid considered is a mixture of very stiff particles (phase P) in a Bingham fluid  (phase S). The shear stress (s) – shear strain (e) relation is expressed by Equation 2 where Equation 1 determines the volume concentration, c, of particles in the composite fluid. V denotes volume.  Subscripts P and S refer to particle phase and matrix phase S respectively.

Formally the original- and the composite (or generalized) Bingham expression, see [3], look alike. The viscosity (() of the material first becomes active when the matrix (fluid) stress exceeds the matrix yield stress SS.

Composite geometry

The composite geometry (particle shape and size distribution) is considered in Equation 2 by the so-called geometry function ((() expressed by Equation 3 with shape functions ((P,(S), expressed by Equation 4 and illustrated in Figure 1.

Principal parameters for the description of geometry in this paper are aspect ratio (A = length/diameter) and the critical concentration cS of ellipsoidal particles considered (cS ( maximum packing density ( eigenpacking). Normally, we may expect improved quality of particle size distribution (smoothness and density) to be associated with higher cS.

Geo-function	                   (3)

The so-called shape factors, (oP, (oS, appearing in Equation 4 are determined by Equation 5.

(4)

Shape factor                 (5)

Normally an interaction power of M = 1 is used in composite analysis assuming a 'moderately' increasing state of interaction between aggregates at increasing concentration. Lower interaction and higher interaction can be described with M < 1 and M > 1 respectively. Unless otherwise stated, a moderate interaction with M = 1 is used in this paper. If otherwise stated MS and MV indicate interaction powers used in yield stress analysis and in viscosity analysis respectively.

Figure 1. Shape functions (μP,μS) with M = 1 and critical concentration cS (concentration of solid phase in a pile of particles).

Figure 2. Spherical particles (A = 1) in a viscous matrix. Present analysis and empirical descriptions by Eilers and Brinkman.

Theory and experiments

As can be seen from Figure 2, reproduced from [1], the relative viscosity predicted by Equation 2 agrees with a solution developed by Einstein [4] in his study of the viscosity of dilute sugar solutions. The expression also agrees with data obtained from experiments on mixtures made of fluids with finite particle concentrations. Two empirical descriptions (Eilers and Brinkman), reported in [5,6,1] for such data are also shown in Figure 2. At the Technical University of Denmark an experimental study has recently been made on the influence of coarse aggregates on the rheology of fresh concrete. The study is reported in [7] from which the results presented in Figures 3 and 4 are reproduced.

Figure 3. Viscosity of concrete as related to volume fraction of coarse aggregates [7]. Solid lines are predicted with MV = 1. Mortar viscosity is (S = 2.5 Pa*sec. cS  = 0.65.

Figure 4. Yield stress of concrete as related to volume fraction of coarse aggregates [7]. Solid lines are predicted with MS = 3.5. Mortar yield stress is SS = 1 Pa. cS  = 0.65.

Conclusion

The well-known Bingham description of the rheology of homogeneous fluids has been generalised in this paper also to include the rheological description of composite fluids. The advantage of such generalisation is obvious: With a few parameters (shape factors, packing density cS, and interaction power M) to describe the composite geometry, only two material properties (viscosity (S, and yield stress SS) of the fluid matrix are required to describe the generalised Bingham behaviour at any composition of the composite fluid considered. The traditional Bingham model needs experimental calibration for any new composition considered

References

- Nielsen, L. Fuglsang: "Rheology of some fluid extreme composites – such as fresh self-compacting concrete“, Nordic Concrete Research, 2(2001), 83 – 93.

- deLarrard, F.: “Concrete Mixtures Proportioning: A Scientific Approach”, Modern Concrete Technology Series, E&FN SPON, London 1999.

- Bingham, E.C.: "An investigation of the laws of plastic flow", Bur. of Standards Bull., 13(1916), 309. 'Colloid types', Fifth Coll. Symp. Monograph, 1(1928), 219.

- Einstein, A.: "Eine neue Bestimmung der Moleküldimensionen", An. Physik, 19(1906), 289 and 34(1911), 104.

- Holliday, L. (ed): "Composite materials", Elsevier Publishing Company, New York, 1966, (p. 34, Chapter on Inclusions in a Viscous Matrix).

- Eirich, R.F. (ed): "Rheology, Theory and Applications", Academic Press Inc., New York, 1958, (p. 363, Chapter on Rheological Properties of Asphalt).

- Geiker, M.R., Brandl, M., Thrane, L. Nyholm, and Nielsen, L. Fuglsang: “Effect of coarse aggregate fraction and shape on the rheological properties of self-compacting concrete”. Cement, Concrete, and Aggregates, Vol. 24, No. 1, June 2002.

# Footnotes

)	The electronic version of this reference should be preferred. Due to a number of printing errors the paper version is very difficult to read.

2)	A software SCCFINAL has been developed to consider the rheology of fresh concrete. It can be downloaded from http://www.byg.dtu.dk/publisering/software_d.htm.